## Slide 1: Quenched Bond Disorder in Non-Collinear Magnets
Santanu Dey
Technische Universität Dresden

## Slide 2: Content
Quenched disorder: Random fields
  Random fields and the Imry-Ma criterion.
  Separate lower critical dimension for discrete and continuous symmetry.
Quenched disorder: Random couplings
  Bond disorder in frustrated non-collinear magnets.
  Rigid in-commensurability domains.
An example
  Disordered triangular lattice Heisenberg antiferromagnet.
  Experiments on related systems

## Slide 3: Quenched Disorder: Random Fields
Lower critical dimensions

## Slide 4: Random fields and the Imry-Ma criterion
      In the absence of random fields,
      Due to Ising symmetry no energy
      change in the bulk.
      But a finite energy cost at
      the surface of the domain
      wall
A simple picture with Ising spins:

## Slide 5: Random fields and the Imry-Ma criterion
      In the presence of random fields,
      but this time the bulk energy is affected.
      The energy cost is the same
A “typical value” for
possible energy gain.
A simple picture with Ising spins:

## Slide 6: Random fields and the Imry-Ma criterion
      In the presence of random fields,
      long range order is destroyed if,
      This makes
      the lower
      critical dimension for discrete symmetries.
Favoured!
Y. Imry and S.-k. Ma, Phys. Rev. Lett. 35, 1399 (1975)
G. Grinstein and Shang-keng Ma, Phys. Rev. Lett. 49, 685 (1982)
A simple picture with Ising spins:

## Slide 7: Random fields and the Imry-Ma criterion
[1] E. Pytte, Y. Imry, and D. Mukamel,Phys. Rev. Lett. 46, 1173 (1981)
[2] K. Binder, Y. Imry, and E. Pytte, Phys. Rev. B 24, 6736(R) (1981)
[3] G. Grinstein and Shang-keng Ma, Phys. Rev. Lett. 49, 685 (1982)
Rough domain walls:
Domain walls can be rough and ill defined
Domain wall thickness scales as,
implying that for domain walls thickness, , which, once included in the energy estimate gives a critical dimension,
[1,2]
But an even more careful analysis shows that the scaling is in fact,
for , the ratio , implying, [3]

## Slide 8: Random fields and the Imry-Ma criterion
      A random field Heisenberg model for illustration,
      Order parameter can smoothly vary
      between domains, costing less
      energy
      So the lower critical dimension
      for continuous symmetries is,
Y. Imry and S.-k. Ma, Phys. Rev. Lett. 35, 1399 (1975)
For continuous symmetries:

## Slide 9: Random fields and the Imry-Ma criterion
The order parameter field couples with the random fields,
This leads order parameter fluctuation
infrared divergent for
Hence, the lower critical dimension for random field systems with continuous symmetry is,
Goldstone modes and infrared divergence:
Goldstone modes,
Y. Imry and S.-k. Ma, Phys. Rev. Lett. 35, 1399 (1975)
A. Aharony, Solid State Comm., 28, 8, 667 (1978)

## Slide 10: Quenched Disorder: Random Couplings
Lower critical dimension of disordered non-collinear magnets: Infrared divergence

## Slide 11: Single bond impurity
In a non-collinear Heisenberg antiferromagnet
In a collinear Heisenberg antiferromagnet
Local reorientation for non-collinear magnets
Bond disorder is weaker and it does not break time reversal invariance.

## Slide 12: Single bond impurity
In a non-collinear magnet
In a collinear magnet
There is no change in the bulk order in response to the bond impurity, hence the Hamiltonian is “virtually” unchanged
Local reorientation for non-collinear magnets
Frustration is locally relieved. For infinitesimal disorder, this is a perturbative correction to the “effective” bulk Hamiltonian,

## Slide 13: Single bond impurity
In a non-collinear magnet
Frustration is locally relieved. For infinitesimal disorder, this is a perturbative correction to the “effective” bulk Hamiltonian,
In a linear response approximation this leads to finite expectation value of transverse spin fluctuation.
If we consider the Goldstone modes, , the response is dipolar,
In 2D, the real space response is also dipolar
Dipolar response for the Goldstone modes

## Slide 14: Single bond impurity
Bond impurity: Dipolar response
Vacancy: Octupolar response
Dipolar response in 2D
A. Wollny, L. Fritz, and M. Vojta, Phys. Rev. Lett. 107, 137204 (2011)

## Slide 15: Concentration of bond impurity
Bond impurity: Dipolar response
  For a distribution of random bond impurities,
  For a disordered system, one expects the impurity magnitudes, to be uncorrelated.
The integral diverges for .
Hence the lower critical dimension for bond disordered non-collinear magnets is,
This implies that the transverse correlation has a divergent contribution,
Infrared divergence driven by disorder

## Slide 16: Quenched Disorder: Random Couplings
The Energetics Argument for the Lower Critical Dimension

## Slide 17: Incommensurability domains
Our test system: The triangular lattice Heisenberg model
Claim: In a system with random couplings, some rare regions emerge with a particular bond anisotropy orientation.
In the “isotropic” limit, , the ground state has spiral order with ordering vector,
Incommensurate order in non-collinear magnets
Néel order
Spiral order
A. Yoshimori, J. Phys. Soc. Jpn. 14, 807 (1959)

## Slide 18: Incommensurability domains
Rare regions with particular bond anisotropy:
The surface energy cost for such a domain formation is , while the bulk energy gain is per site as before, . Hence the critical dimension is once again,
In a lattice there is a discrete number of possible bond anisotropy orientation.
In a typical sample they define sharp domain walls
The incommensurate ordering vectors follow the suit
Sharp domain boundaries

## Slide 19: Incommensurability domains at d=2
Disordered triangular lattice Heisenberg model
With

## Slide 20: Incommensurability domains at d=2
Disordered triangular lattice Heisenberg model
With

## Slide 21: Incommensurability domains at d=2
Disordered triangular lattice Heisenberg model
With
Domain size decreases with disorder!

## Slide 22: Properties at the critical dimension
Transverse fluctuation diverges logarithmically at d = 2
The domain size is determined by the condition, , which defines the domain (correlation) length,
This leads to the appearance of order for small values of disorder strength.
Logarithmic divergence

## Slide 23: Properties at the critical dimension
For finite temperature the system will be thermally disordered.
However, for small temperature there will be a competition between thermal and quenched disorder.
At, small T the thermal correlation length is,
[1]
So, the crossover temperature is,
Finite temperature
[1] S. Chakravarty, B. I. Halperin, and D. R. Nelson,Phys. Rev. B 39, 2344 (1989)

## Slide 24: Beyond 2D
If the continuous symmetry of the Hamiltonian is explicitly broken, e.g. an XXZ model, the low energy excitations are gapped, and therefore the transverse fluctuation in the presence of random couplings is given by,
In this case, long range order survives for small disorder with the stability criterion,
Gapped excitations

## Slide 25: Beyond 2D
If the coupling between the layers, is finite then the system has an extra dimension which prevents the divergence and long range order is sustained even in the presence of random couplings. With the bare susceptibility now given by, with
The stability criterion, therefore is given by
Layered quasi-2D system

## Slide 26: An example
Microscopics and experiments on disordered triangular lattice antiferromagnet

## Slide 27: Disordered triangular lattice Heisenberg model
Disordered Heisenberg model
with,
From weak to stronger disorder
  Rectangular distribution,
  Lognormal distribution,
Disorder distribution
Lognormal distribution,

## Slide 28: Disordered triangular lattice Heisenberg model
Classical ground state with iterative local energy minimization.
  Spin-wave expansion on top of disordered classical ground state.
  The Hamiltonian becomes,
  The diagonalization is performed with real space bogoliubov transformation
  The third order terms and the first order terms are combined in a saddle point approximation to give angular fluctuation
Spin-wave theory
  with

## Slide 29: Disordered triangular lattice Heisenberg model
Slave fermion representation to capture the spin singlet formation.
  Decoupling in both singlet and magnetic channel,
  With the mean-field parameters given by,
Mean-field theory
, corresponds to unconstrained Hartree approximation

## Slide 30: Disordered triangular lattice Heisenberg model
Structure factor
Amplifying quantum effects

## Slide 31: Disordered triangular lattice Heisenberg model
Dynamic structure factor
Disordered magnon modes

## Slide 32: Disordered triangular lattice Heisenberg model
Valence bonds at higher disorder
Composite glass

## Slide 33: Disordered triangular lattice Heisenberg model
Valence bonds at higher disorder
Composite glass

## Slide 34: Disordered triangular lattice Heisenberg model
Valence bonds at higher disorder
Composite glass

## Slide 35: Experiments on triangular lattice
Thermal conductivity,
Spin-glass signature in
Magnon modes
Ma et. al, arxiv:1709.00256 (2017)

## Slide 36: Experiments on triangular lattice
Very small non-phonon contribution
1000 times smaller than QSL candidate
It is postulated that disorder induced spin
Glass signature might explain this behavior.
Thermal conductivity,
Spin-glass signature in
Ma et. al, arxiv:1709.00256 (2017)

## Slide 37: Summary
Random bond disorder destroys order in non-collinear magnets below or at the critical dimension 2.
However, relatively large domain sizes at the critical dimension creates a semblance of an ordered phase.
Quantum fluctuation makes the effect of disorder more pronounced.

## Slide 38: Thank you!